## Slide 1
The Importance of Interlayer Bonding in Pavement Construction

## Slide 2: introduction
Why is the topic so important?
Bond Coats and Tack Coats
What is an interlayer bond?
What about waterproofing?
Application

## Slide 3
Dr Stephen Tweed, SHE and Pavement Engineer from the Department for Infrastructure
in Northern Ireland states
“In recognition of the importance on interlayer bonding within pavement structures, the application of bond coat in conjunction with each bituminous layer installed is a current requirement within NI road surfacing contracts. Effective bonding between pavement layers is regarded as a key element in providing more durable, longer lasting assets with lower maintenance requirements, reducing the risk of premature failure resulting from layer delamination or water ingress into the pavement structure. The use of high quality bond coat, between each pavement layer, is considered a fundamental requirement for the delivery of more sustainable pavements with increased service life and whole life value.”
Dr Stephen Tweed, SHE and Pavement Engineer from the Department for Infrastructure
in Northern Ireland states
“In recognition of the importance on interlayer bonding within pavement structures, the application of bond coat in conjunction with each bituminous layer installed is a current requirement within NI road surfacing contracts. Effective bonding between pavement layers is regarded as a key element in providing more durable, longer lasting assets with lower maintenance requirements, reducing the risk of premature failure resulting from layer delamination or water ingress into the pavement structure. The use of high quality bond coat, between each pavement layer, is considered a fundamental requirement for the delivery of more sustainable pavements with increased service life and whole life value.”

## Slide 4: Why is the topic so important?

## Slide 5: Why is the topic so important?

## Slide 6: Why is the topic so important?

## Slide 7: Why is the topic so important?

## Slide 8: Why is the topic so important?

## Slide 9: Why is the topic so important?

## Slide 10: Why is the topic so important?

## Slide 11: Bond Coats and Tack Coats
SHW 900 series - Clause 920
Tack Coats – Relatively low binder content, basic bitumen emulsion
Bond Coats – Relatively low binder content, polymer modified bitumen emulsion. Defined by cohesion levels >1.0J/cm2
Defined by BS EN 13808
Eg
Cationic
Mid point binder content
Presence of bitumen
Polymer modified
Break index class
C
50
B
P
3

## Slide 12: Bond Coats
Generally increased cohesion provides a greater resistance to movement in all dimensions
Enables some relaxation of strain within the bond
Movement here

## Slide 13: Bond coats
Where the binder is picked up on hot tyres, it can carry off onto other areas
2 impacts… - loss of texture where it is dropped off
- removal of bond coat from where it should be

## Slide 14: Bond Coats
“Non Tacky” Bond coats
Resistant to “sticking” to site vehicle tyres
Harder bitumen that is resistant to tyre pick up
Melts into the newly laid asphalt

## Slide 16
Alan Ferguson, former President of the Institute of Asphalt Technology and currently Materials Advisor for Asset Management of Roads in Transport Scotland says
“The proper application of bond coat between all asphalt layers is vital to maximise the life of our asset. Indeed, it is my view that bonding and sealing all asphalt layers combined with the correct level of compaction results in a structural layer that can significantly exceed design life. “

## Slide 17: What constitutes an interlayer bond?
Surface Course
Binder Course
Base Course
Well bonded structure effectively spreading stress
Traffic Force
“Monolithic Structure”
Good
Interlayer
Bonding

## Slide 18: What constitutes an interlayer bond?
Tension
Tension
Strain
Traffic Force
Poorly bonded structure
Premature development of Fatigue cracking (alligator cracking)

## Slide 19: What constitutes an interlayer bond?
Shear Force
Shear force
Strain
Traffic Force
Poorly bonded structure
Development longitudinal wheel track cracking)

## Slide 20: Research evidence
There is plenty of evidence that unbonded structures reduce the life of the Pavement significantly
Roffe and Chaignon in 2002 suggested that 60% loss of pavement life can be expected
Peattie in 1980 completed a report illustrating the high number of sites failing due to poor interlayer bonding
NCAT have modelled the phenomenon previously discussed where they illustrated the independent movement of the surfacing layer led to early cracking failure

## Slide 21: Water impact
Well bonded structure inhibits water going through structure and getting into lower layers
If water comes laterally it stops migration through the structure

## Slide 22
Stuart Evans, Pavement Manager, from the Department for Economy and Infrastructure for the Welsh Government
“Full bonding coverage of surfaces between interlayers has been a critical requirement in the drive to improve the quality of Welsh Government surfacing works. Recurring issues such as de-bonding, joint failure, water ingress and the rapid deterioration of mats in winter months are all symptomatic of insufficient bond coat application. Increasing rainfall levels and temperature variability are challenges we face over future years - desirable design life can only be attained by good quality control and thorough bond coat application”
Stuart Evans, Pavement Manager, from the Department for Economy and Infrastructure for the Welsh Government
“Full bonding coverage of surfaces between interlayers has been a critical requirement in the drive to improve the quality of Welsh Government surfacing works. Recurring issues such as de-bonding, joint failure, water ingress and the rapid deterioration of mats in winter months are all symptomatic of insufficient bond coat application. Increasing rainfall levels and temperature variability are challenges we face over future years - desirable design life can only be attained by good quality control and thorough bond coat application”

## Slide 23: Application – BS 594987

## Slide 24
Asphalt Layer
Asphalt Layer
Asphalt Layer
X
X

Application – BS 594987
< 0.2l/m2 residual
Inadequate free bitumen available to bond the layers
Inadequate free bitumen to waterproof
Significantly > 0.35l/m2 residual
Excess of bitumen potentially creating a “slip plane”
Potential bleed through of binder on asphalt application

## Slide 25: Application
Bond Coat application – Not tack coat (only by exception)
Machine laid – Not hand laid (only by exception)
Accurately control the ROS
Pre work check of “Tray Test BS 1707” to validate eveness of spray
Tested on site via carpet tile test for ROS

## Slide 26
Desirable application –
Uniform across the mat

## Slide 27
Undesirable – inconsistent application

## Slide 28: application
Potential issue is the “complete break” of the emulsion
Contracts with night-time work and restricted access
Critical to maintain the required application rate
Stability is weather dependent

## Slide 29: The future
Significant challenges coming up that will potentially make bonding and waterproofing even more critical
Intense wet
periods
More temperature extremes
Electric vehicles
Driverless vehicles
Etc etc….

## Slide 30
Arash Khojinian, Head of Pavements for Highways England, says:
“Increasing the durability of the pavements on England’s strategic road network is vital. Properly bonded, well-designed asphalt layers are key to building longer-lasting pavements. Not only does the bond coat create a single uniform structure of the pavement, but it plays a critical role in protecting the lower layers from ingress of water. Correct specification and application of bond coats is essential if we want to see long-term improvement in the quality of England’s motorways and major roads”.
Arash Khojinian, Head of Pavements for Highways England, says:
“Increasing the durability of the pavements on England’s strategic road network is vital. Properly bonded, well-designed asphalt layers are key to building longer-lasting pavements. Not only does the bond coat create a single uniform structure of the pavement, but it plays a critical role in protecting the lower layers from ingress of water. Correct specification and application of bond coats is essential if we want to see long-term improvement in the quality of England’s motorways and major roads”.

## Slide 31
MAKE IT HAPPEN!
Execute
Design
Control
Specify
www.rea.org.uk
www.rsta-uk.org